## Slide 1: CEDVs calculation using MathCad
Outline
Basic concept
Required data
Program structure
Step-by-step guide
Advanced settings

## Slide 2: Current integration based fuel-gauging
Battery is fully charged
During discharge capacity is integrated
State of charge (SOC) at each moment is Q/Qmax
Qmax is updated every time full discharge occurs
Q
SOC=Q/Qmax

## Slide 3: Learning before fully discharged
It is too late to learn when 0% capacity is reached
We can set voltage threshold that correspond to given percentage of remaining capacity
However, true voltage corresponding to 7% depends on current and temperature
0
1
2
3
4
5
6
3
3.5
4
4.5
Capacity, Ah
Voltage, V
EDV0
Q
max
0%
3%
7%
EDV1
EDV2

## Slide 4: Learning before fully discharged with current and temperature compensation
Modeling last part of discharge allows to calculate function V(SOC, I, T)
Substituting SOC=7% allows to calculate in real time CEDV2 threshold that corresponds to 7% capacity at any current and temperature
0
1
2
3
4
5
6
3
3.5
4
4.5
Capacity, Ah
Voltage, V
Q
max
7%
CEDV2 (I2)
CEDV2 (I1)

## Slide 5: Basic functionality of CEDV parameters
Parameters EMF and C0 define function OCV(SOC,T)
Parameters (R0,R1 and T0) define R(SOC,T). R1 defines the slope of R(SOC) dependence, R0 the magnitude of R, and T0 the slope of R(T) dependence.
Parameter TC defines additional resistance increase at temperatures below 21oC: R`(SOC,T).
Parameter C1 allows to shift whole function to the left. EDV2 is reached earlier and so reserve capacity is provided. 1 Unit of C1 shifts function by 0.39%
Battery Low
EDV2
OCV(SOC,T)
OCV(SOC,T)-I*R(SOC,T)
OCV(SOC,T)+I*R`(SOC,T)

## Slide 6: Required data
Continious discharge at 2 different rates, from fully charged state until termination voltage is reached.
Time, voltage, current and temperature (directly on the cells) has to be recorded and stored as separate columsn. Any text should be removed from files prior to calculations.
Easy recording method is to use our EV software that is reading data directly from our fuel-gauge.
Make sure to set over-temperature limits in the fuel-gauge higher then expected cell temperature during the test.
First rate should be average typical, and second should be average high for your application. Note that high rate should NOT be maximal peak current, but maximal average sustained rate that can practically occur in the application.
Discharge does not have to be constant current. It can be any load pattern typical for your application, including constant power.
Battery should be fully charged prior to application of test pattern.
Test at both rates has to be perfored at 3 different temperatures. Typical temperatures for the test are 5, 30, 50 oC. Note that cells heat-up during high rate discharge, so if your max spec temperature is 70, you can use chamber temperature 50.
As result of all tests you will obtain 6 files.
If temperature was changed, battery should be left for reaching thermal equilibrium for at least 2 hrs prior to testing

## Slide 7: Short calculation guide (1)

## Slide 8: Short calculation guide (2)

## Slide 9: Short calculation guide (3)

## Slide 10: Program structure
User parameters input
Experimental data reading and pre-processing to produce standardized SOC,V,T,I matrixes
Linear fit of the data to produce initial guess for CEDV parameters
Non-linear fit of the data to produce final parameters achieving best fit of all loads and temperature data
Modify EDV TC to achieve best fit of low-temperature data
Reviewing of fit quality and resulting parameters

## Slide 11: User parameter input
Usage related parameters:
Reserve capacity Q_reserve defines how much capacity will be left when EDV0 is detected by GG
EDV is the termination voltage for single cell
SN is number of serial cells
Data columns assignment
To be changed if new data format is used. Uses zero-origin, so the first column of the file will have index 0
Additional parameters (usually no need to change):
Only part of voltage profile is modeled by CEDV parameters. SOClim defines how much percent of SOC from the end will be covered.
Voltage profile very near the end of charge is distorted. SOCmin defines how much (% of SOC) from the end has to be dropped

## Slide 12: Experimental data reading and pre-processing to produce standardized SOC,V,T,I matrixes
Reading and processing normal temperature file
Assign matrixes A to low-load data, B2 to middle-load and B to high load data
Reading and processing high temperature file
Assign matrixes C2 to middle-load and C to high load data
Reading and processing low temperature file
Assign matrixes D2 to middle-load and D to high load data

## Slide 13: Assignment of arrays: which current level to use
There is a choice which current level (middle/second or maximal/third) to use for linear fit determining of R(SOC,T) defining parameters
Usually the maximal gives best results and gives more conservative estimate.
Subsequent non-linear fit will use both current data
Data-parsing routine places the voltages at the end of each level in arrays OUT1 (low), OUT2 (middle) and OUT3 (max).
To use middle current, assign second array to arrays B, C and D as B:=OUT2, C:=OUT2 and D:=OUT2, And B2=OUT3, C2=OUT3, D2:=OUT3
To use maximal current (default), assign third array to arrays B,C and D as B:=OUT3, C:=OUT3, D:=OUT3, And B2=OUT2, C2:=OUT2,D2:=OUT2
Set I=curr[2]*1000 (located after file loading section) to use maximal current, or I=curr[1]*1000 for middle current level.

## Slide 14: Reading and processing data-file: section structure
Read t,V,I,T data from assigned columns of data-file
Find the end of charge, and remove charging part of data
Detect currents of each current level
Find indexes of data-points at the end of each pulse.
Calculate charge passed until EDV is reached, Qmax
Calculate SOC for all data-points based on Qmax
Find first and last indexes which are in the SOC region of interest
Assign values of data-points at the end of each pulse in region of interest to output arrays

## Slide 15: Linear fit of the data to produce initial guess for CEDV parameters
Finding EMF and C0 parameters
Finding R1 parameter
Finding R0 and T0 parameters

## Slide 16: Finding EMF and C0 parameters
Transform low-rate data for normal temperature (matrix A) into form with makes OCV(SOC,T) equation linear in terms of EMF and C0 parameters
Linear fit the transformed data to obtain EMF and C0
Alternatively:
Use generic EMF and C0 parameters obtained from true open-circuit voltage measurements.

## Slide 17: Finding R1 parameter
Calculate deviation of measured voltage at high rate (matrix C) from calculation based on no-load assumption, err1 array
Assuming that err1 is equal to I*R drop, linear fit the R(SOC) equation to this data find R1 (slope of R(SOC) dependence

## Slide 18: Finding R0 and T0 parameters
Modify the err1 data (high rate) so that R(SOC,T) equation becomes linear 2-dimensional equation in terms of R0 and T0
Use 2-dimensional linear regression of modified data to find R0 and T0.

## Slide 19: Non-linear fit of the data to produce final parameters achieving best fit of all loads and temperature data
Choice: to fit all temperatures or exclude low temperature. Later usually works better because low-temperature case can be additionally corrected by TC
Non linear fit:
  All equations are combined into one V(EMF, C0,R0,R1,T0)
  First derivatives of vs each parameters are defined
  Full-Newton non-linear fit is used for find optimal parameters

## Slide 20: Non-linear fit of the data to produce final parameters achieving best fit of all loads and temperature data

## Slide 21: Reading the results
To execute calculation, place the cursor end of work-sheet, and press F-9. Or, from Math menu execute “calculate worksheet” command.
Read CEDV parameters at the last page
Note that EMF and EDVR0 parameters have to be divided by number of serial cells before writing to the flash if EDVV parameter in pack configuration is set to 0.
Graph shows the fit of the program voltage
CEDV parameters can be saved into a data-file. Change the file name in WRITEPRN statement. File is readable by validation program LOGVER

## Slide 22: What can go wrong? Fit not close enough
Fit is considered good if voltage at 7% fit is not more then 2% far along X axes from same voltage on experimental curve. If not satisfactory try following:
Increase EDVTC value here (but not higher then 11):
Check that data format is correct, e.g. column assignment is correct, units of resulting B,C,D arrays are %,Volt, degree K, Ampere)
Check that current sign is correct (last column in B,C,D arrays is positive)
decrease, change fitting range by modifying SOCmin and SOCmax
If EDVC1 fitting is disabled (as shown in two subsequent slides), try enabling it.

## Slide 23: What can go wrong? Negative parameter values.
Non linear fit might produce negative values for some parameters. In this case:
  Check that data format is correct, e.g. column assignent is correct, units of resulting B,C,D arrays are %,Volt, degree K, Ampere)
  Check that current sign is correct (last column in B,C,D arrays is positive)
  decrease, change fitting range by modifying SOCmin and SOCmax
If above did not help, disable fitting of EDVC1. To do this, click on the right side of this line:
Go to the line “selection of fit options”. Right-click on both statement, select “disable evaluation”.
Black square will appear in upper right corner

## Slide 24: What can go wrong? Negative parameter values (cont.)
Scroll down and right click on statements below. Select “enable evaluation”. Black square will disappear in upper right corner
Additionally, scroll down and right click on statements below. Select “disable evaluation”. Black square will appear in upper right corner